## Slide 1: Performance Characterization of Porous Silicon (PoSi) Schottky Devices
Nick Kantack
V. R. Whiteside, Y. Cheng, N. Shahabi Sani, L. A. Bumm, and I. R. Sellers
4/16/2016

## Slide 2: Motivation
Solar energy
  Cheap
  Efficient
  Versatile
Silicon is the most established of all solar technologies.
Innovations for silicon cells can apply to other emerging solar materials
Porous silicon reduces reflection, the primary loss separating current cells from ideal performance.

## Slide 3: Research Summary
The nature of PoSi devices fabricated at OU are not fully understood.
Would like to know:
  What charge transport models dominate?
  What loss mechanisms dominate?
  What is the quality of the devices?
  How do they compare to non-porous silicon?
PoSi Cells
Si Cells
Pd
Si/PoSi
Al
Quantum14 Inc. Kajino-cho, Koganei-shi, Tokyo
SEM of Porous Silicon
Device Structure

## Slide 4: Discussion of Reflectivity
Porous silicon schottky devices demonstrated ~25% lower reflectivity.
Light entering the pores impinges the walls multiple times, increasing probability of absorption.
Reflectivity is high in these devices due to Palladium layer.
Chart: Reflectivity of Silicon device vs. Porous Silicon device

## Slide 5: Theory Of Device Performance
A Schottky Diode uses a metal-semiconductor interface, in our case Palladium joining an N-type Silicon layer (porous or non-porous).
P Type
Semiconductor
N Type
Semiconductor
Bandgap
N Type
Semiconductor
Metal
Schottky Barrier

## Slide 6: IV Characterization
Observe device properties an non-idealities in a standardized way
  Diode behavior
  Ohmic behavior

## Slide 7: Measuring IV Performance
Discernable diodic behavior from all samples
Ohmic leakage current evident in samples (constant slope), indicating density of shunt paths.

## Slide 8: Thermionic Emission Model
Charge across the junction in terms of kinetic energy.
The temperature of the device affects the distribution of kinetic energies among carriers.
N Type
Semiconductor
Metal

## Slide 9: Temperature Dependent IV Characterization
Temperature dependence taken from 77K to 350K at 10K steps. Saturation current and fill factor change smoothly with temperature.
Temp (K)
Chart: Thermal Oxide Treated PoSi Schottky IV at Various Temperatures
| -1.5 | -1.4 | -1.3 | -1.2 | -1.1000000000000001 | -1 | -0.9 | -0.8 | -0.7 | -0.6 | -0.5 | -0.4 | -0.3 | -0.2 | -0.1 | 1.9429E-16 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5
77 | -4.2532 | -4.2863 | -4.3219 | -4.3597 | -4.3987 | -4.4404 | -4.4859 | -4.535 | -4.5904 | -4.6591 | -4.7628 | -4.9445 | -5.2383 | -5.7162 | -6.6835 | -9.0561 | -7.0452 | -5.6683 | -4.6174 | -3.4978 | -1.8908 | -0.071024 | 1.2237 | 1.9588 | 2.4328 | 2.7839 | 3.0588 | 3.2851 | 3.4791 | 3.6468 | 3.7936
80 | -4.2672 | -4.2989 | -4.3319 | -4.3675 | -4.4046 | -4.4448 | -4.4891 | -4.5366 | -4.5908 | -4.6575 | -4.7582 | -4.9375 | -5.2304 | -5.7068 | -6.6681 | -9.048 | -6.9835 | -5.6685 | -4.6334 | -3.4842 | -1.8407 | 0.0070749 | 1.271 | 1.9918 | 2.4732 | 2.8283 | 3.1079 | 3.3384 | 3.5359 | 3.7078 | 3.863
90 | -4.3437 | -4.3775 | -4.4132 | -4.4499 | -4.4893 | -4.5304 | -4.5747 | -4.6241 | -4.6786 | -4.7428 | -4.8328 | -4.9897 | -5.2589 | -5.7137 | -6.657 | -9.0409 | -6.9657 | -5.6431 | -4.5782 | -3.3678 | -1.6767 | 0.23341 | 1.4451 | 2.146 | 2.6206 | 2.9739 | 3.2522 | 3.4811 | 3.6747 | 3.842 | 3.9892
100 | -4.3442 | -4.3772 | -4.4116 | -4.4472 | -4.4862 | -4.5276 | -4.5705 | -4.6191 | -4.6727 | -4.736 | -4.8252 | -4.9827 | -5.2515 | -5.7046 | -6.6388 | -9.0384 | -7.0039 | -5.6264 | -4.5628 | -3.3289 | -1.6269 | 0.28893 | 1.4761 | 2.1655 | 2.6343 | 2.9845 | 3.2611 | 3.489 | 3.6813 | 3.848 | 3.995
110 | -4.4038 | -4.4399 | -4.4749 | -4.5127 | -4.5518 | -4.5969 | -4.6374 | -4.6907 | -4.744 | -4.8097 | -4.8917 | -5.033 | -5.2756 | -5.7076 | -6.6122 | -9.0822 | -6.944 | -5.4844 | -4.4129 | -3.1716 | -1.4577 | 0.44276 | 1.5531 | 2.207 | 2.6572 | 2.9962 | 3.2654 | 3.4883 | 3.6775 | 3.8413 | 3.9859
120 | -4.0537 | -3.9852 | -4.0626 | -4.1317 | -4.1361 | -4.251 | -4.2858 | -4.3076 | -4.3317 | -4.4657 | -4.5856 | -4.739 | -5.0307 | -5.4421 | -6.2755 | -9.0076 | -6.3521 | -5.1447 | -4.1633 | -3.0215 | -1.3577 | 0.51581 | 1.5914 | 2.2271 | 2.667 | 2.996 | 3.2612 | 3.4812 | 3.6689 | 3.8313 | 3.9749
130 | -4.4066 | -4.4461 | -4.4888 | -4.5306 | -4.5744 | -4.6189 | -4.6657 | -4.7156 | -4.7699 | -4.8341 | -4.914 | -5.0389 | -5.2589 | -5.662 | -6.5363 | -9.0243 | -6.7582 | -5.4412 | -4.302 | -2.978 | -1.1719 | 0.68183 | 1.6911 | 2.2999 | 2.7267 | 3.0521 | 3.3127 | 3.5296 | 3.7146 | 3.8753 | 4.0175
140 | -4.3774 | -4.4168 | -4.4593 | -4.5022 | -4.5459 | -4.5901 | -4.6375 | -4.6889 | -4.7431 | -4.8057 | -4.8839 | -5.0083 | -5.2283 | -5.6265 | -6.4895 | -9.0189 | -6.8835 | -5.3702 | -4.227 | -2.892 | -1.0575 | 0.76723 | 1.7463 | 2.3424 | 2.7648 | 3.0881 | 3.3479 | 3.5644 | 3.7494 | 3.9113 | 4.0552
150 | -4.2981 | -4.3117 | -4.361 | -4.4026 | -4.4431 | -4.5021 | -4.5578 | -4.5992 | -4.6534 | -4.7329 | -4.8112 | -4.9413 | -5.1453 | -5.5319 | -6.3595 | -8.9873 | -6.5074 | -5.2133 | -4.0608 | -2.695 | -0.79343 | 0.93946 | 1.8535 | 2.4208 | 2.8258 | 3.1385 | 3.3913 | 3.6032 | 3.7847 | 3.943 | 4.0835
160 | -4.3114 | -4.3496 | -4.3901 | -4.4302 | -4.4709 | -4.5208 | -4.5708 | -4.6213 | -4.6764 | -4.7404 | -4.8205 | -4.9403 | -5.1451 | -5.5258 | -6.3506 | -8.9882 | -6.5181 | -5.1932 | -3.9877 | -2.5782 | -0.62626 | 1.0409 | 1.9183 | 2.4691 | 2.8649 | 3.1721 | 3.4215 | 3.631 | 3.8109 | 3.9682 | 4.1079
170 | -4.2132 | -4.2656 | -4.3196 | -4.3703 | -4.4221 | -4.4783 | -4.5313 | -4.5868 | -4.6495 | -4.7209 | -4.8023 | -4.9195 | -5.1144 | -5.4757 | -6.2674 | -8.9255 | -6.4145 | -5.0815 | -3.8339 | -2.3719 | -0.36348 | 1.1761 | 1.9931 | 2.515 | 2.8937 | 3.1896 | 3.431 | 3.6348 | 3.8104 | 3.9643 | 4.1013
180 | -4.1557 | -4.2072 | -4.2607 | -4.3138 | -4.3691 | -4.4252 | -4.48 | -4.5398 | -4.6034 | -4.6751 | -4.7601 | -4.8832 | -5.0837 | -5.4438 | -6.2226 | -8.953 | -6.3602 | -5.0162 | -3.7359 | -2.2476 | -0.21516 | 1.2611 | 2.0518 | 2.5618 | 2.9338 | 3.2254 | 3.4638 | 3.6657 | 3.8399 | 3.9922 | 4.1286

## Slide 10: Expanded Model
The following equation models metal-semiconductor-metal lead selenide diodes.
I adapted this equation to incorporate the resistivity elements into an expanded diode equation.
Daniel Bozyigiti, et. al. “A quantitative model for charge carrier transport, trapping and recombination in nanocrystal-based solar cells”

## Slide 11: Fitting the IVs: Expanded Model
The expanded model largely explains the current observed in the devices.
Chart: Dark IV of Silicon at 300K
| -1.5 | -1.4 | -1.3 | -1.2 | -1.1000000000000001 | -1 | -0.9 | -0.8 | -0.7 | -0.6 | -0.5 | -0.4 | -0.3 | -0.2 | -0.1 | 1.94E-16 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
Data | -2.2136 | -2.2728 | -2.3343 | -2.399 | -2.468 | -2.5416 | -2.6208 | -2.7057 | -2.8001 | -2.9115 | -3.0448 | -3.2091 | -3.4253 | -3.733 | -4.3124 | -3.7088 | -2.2984 | -0.939 | 0.55813 | 1.6147 | 2.2635 | 2.7132 | 3.0515 | 3.3202 | 3.5419
Model | -1.9055 | -1.9742 | -2.048 | -2.1277 | -2.2142 | -2.309 | -2.4137 | -2.5307 | -2.6632 | -2.816 | -2.9964 | -3.2166 | -3.4996 | -3.8961 | -4.5687 | -4.3208 | -3.0656 | -1.5424 | 0.14678 | 1.5479 | 2.3373 | 2.7389 | 3.0284 | 3.2945 | 3.5562
Offset likely due to omission of voltage lowering

## Slide 12: Extracting Constants
Arrhenius Saturation Current is linear with inverse temperature.
  Intercept - Richardson Constant
  Slope - Barrier Height
Barrier Heights (eV) |  | 
Non-porous | Porous | ThermalO
0.34 | 0.25 | 0.31

## Slide 13: Conclusions
Identified a compelling diode model incorporating resistivity effects
Observed results consistent with thermionic emission theory
Determined physical constants about device characteristics from the fitting constants
  Barrier height
  Richardson Constant

## Slide 14: Future Work
Perform this analysis on new cells from OU
  Standardize the cell area
  Test in conjunction with quantum dots
Better understand deviations from model
  Tunneling current in reverse bias?

## Slide 15: Acknowledgements
Dr. Ian Sellers
Dr. Vincent Whiteside
Dr. Lloyd Bumm and the Bumm Group
Fellow researcher group members
Partners of the Oklahoma NASA Energy and Materials Symposium, and the University of Tulsa for hosting the event
Oklahoma Center for the Advancement of Science & Technology
  OARs program grant number # AR 14-041